|  | SCIENTIFIC & PRODUCTION COMPANY «BARS-2» |
| --- | --- |
| Optikov str., 4, St-Petersburg, 197374, Russia tel./fax: +7 (812) 346 78 82, 346 78 83 tel.: +7 (812) 346 78 91, 346 78 92/93/94/96 http: www.bars2.com E-mail: bars2@ bars2.com | TECHNICAL DATA SHEET |
|  | Revision 21/02/2018 |
|  | Print date 11/5/2019 |

| DESCRIPTION |
| --- |
| PRODUCT NAME | BASCO® DESSICANT MASTERBATCH |
| PRODUCT CODE: | T0035/09-PE |
| COLOR: | UNCOLORED, NON-TRANSPARENT |
| PHYSICAL PROPERTIES |
| CARRIER RESIN |  |
| TYPE: | LDPE |
| DENSITY: | 915-920 kg/m3 |
| MELT FLOW RATE | 7-8 (190°/2.16 kg) |
| MASTERBATCH |  |
| BULK DENSITY: | 700-720 kg/m3 |
| MELT FLOW RATE | 3-5 (190°/2.16 kg) |
| ADDITIVE: | DRYING AGENT |
| ADDITIVE LOADING | 60 % |
| MAXIMUM PROCESSING TEMPERATURE | 260°C |
| LIGHT FASTNESS | 8 |
| APPLICATION: |
| MB T0035/09-PE IS USED FOR PROCESSING OF WET RAW MATERIALS (LDPE, HDPE, LLDPE, PP, ABS, PVC), ESPECIALLY RECYCLES. THE MB CONTAINS THE ACTIVE DRYING AGENT WHICH ABSORBS LARGE AMOUNTS OF WATER, AND INPUT 0.5-3% OF THE MB ALLOWS GETTING THE QUALITY PRODUCTS (FILMS, TAPES, TUBES, MOLDED GOODS ETC.) EVEN IN CASE OF USING OF THE FEEDSTOCK WITH HIGH WET CONTENT. FURTHERMORE, THE DESICCANT MB WHEN USED IN THE PROCESSING OF RECYCLED PVC, NOT ONLY ABSORBS MOISTURE, BUT ALSO ABSORBS ACIDIC PRODUCTS OF THE DEGRADATION OF PVC. |
| REMARKS: |  |
| RECOMMENDED DOSAGE | 0.5-5 % |
| THE EXACT DOSAGE SHOULD BE DETERMINED ACCORDING TO CUSTOMER’S RAW MATERIALS, EQUIPMENT AND REQUIREMENTS TO THE FILMS. |
| PERFORMANCE OF MB T0035/09-PE IS INFLUENCED BY POLYMER, PROCESSING CONDITIONS AND THICKNESS OF THE GOODS |
| MB T0035/09-PE HAS STATE REGISTRATION FORM OF CUSTOM UNION (RUSSIAN FOOD CONTACT APPROVAL) № RU.78.01.06.008.E.005321.08.11 |
| MB T0035/09-PE IS FREE FROM HEAVY METALS AND DANGEROUS SUBSTANCES ACCORDING SVHC LIST |
| MB T0035/09-PE EXPECTED SHELF LIFE IS 2 YEARS IF STORED PROPERLY IN WARM DRY CONDITIONS. OPENED BAGS OF THE MB AFTER USE MUST BE SEALED AS SOON AS POSSIBLE |